## Slide 1: The Atlung Method for Intercalant Diffusion and Resistance (AMIDR) A Complete Pulse Method for Measuring Cathode Solid-State Diffusivity
AMIDR = Sequel to AMID

## Slide 2: Cell Impedance
Impedance can come from many parts of the cell
Impedance limits power density (and energy density if capacity is kinetically hindered)
Cathode active material is AMIDR’s focus
Li+ electrolyte @ separator
Li+ cathode interface
Li+ cathode diffusion
Cathode
Li+ electrolyte @ cathode
Li+ anode interface
Li+ anode diffusion
Anode
Li+ electrolyte @ anode
e- wire
e- anode
e- cathode

## Slide 3: Diffusivity Reproducibility
Diffusivity is difficult to measure accurately
Diffusion impedance develops over long time scales
Many methods require significant mathematical approximations ()
Figure adapted from [1] S. Kang and W. Chueh, “GITT Reinvented” J. Electrohem. Soc., 168, 120504 (2021)
Diffusion
Interface

## Slide 4: How to Measure Diffusivity Accurately
Everything needs to be done right for accurate diffusivity measurements
“A chain is only as strong as its weakest link”
AMIDR does nearly all of it for you (available at github.com/MitchBall/AMIDR)
Cell Tester
Protocol
Model
Rapid Pulse Initiation
High Sampling Rate
“Complete” Finite-volume
Resistance Inclusion
Small V Limit Pulses
Normalized Error
“Complete” Pulses/Rests
Side Reaction Detection
Logarithmic Sampling
Shielding
Inconsistent Detection
Cell Design
Ultra-low Mass Loading
Charge/Discharge Agreement
Error Management
Reference Electrode
“Incomplete” Pulse Detection

## Slide 5: Cell Design
Intelligent cell design eliminates some sources of impedance and amplifies desired sources
Reference electrode (~0.31 V vs Li+/Li0) eliminates anode impedance
Ultra-low mass loading removes electrolyte @ cathode impedance and amplifies diffusion and interface
Li+ electrolyte @ separator
Li+ cathode interface
Li+ cathode diffusion
Cathode
Li+ electrolyte @ cathode
Li+ anode interface
Li+ anode diffusion
Anode
Li+ electrolyte @ anode
e- wire
e- anode
e- cathode

## Slide 6: Cell Design
Intelligent cell design eliminates some sources of impedance and amplifies desired sources
Reference electrode (~0.31 V vs Li+/Li0) eliminates anode impedance
Ultra-low mass loading removes electrolyte @ cathode impedance and amplifies diffusion and interface
Li+ electrolyte @ separator
Li+ cathode interface
Li+ cathode diffusion
Cathode
Li+ electrolyte @ cathode
Li+ anode interface
Li+ anode diffusion
Anode
Li+ electrolyte @ anode
e- wire
e- anode
e- cathode

## Slide 7: Cell Design
Intelligent cell design eliminates some sources of impedance and amplifies desired sources
Reference electrode (~0.31 V vs Li+/Li0) eliminates anode impedance
Ultra-low mass loading removes electrolyte @ cathode impedance and amplifies diffusion and interface
Li+ electrolyte @ separator
Cathode
Li+ electrolyte @ cathode
Li+ anode interface
Li+ anode diffusion
Anode
Li+ electrolyte @ anode
e- wire
e- anode
e- cathode
Li+ cathode interface
Li+ cathode diffusion

## Slide 8: Cell Design
Intelligent cell design eliminates some sources of impedance and amplifies desired sources
Reference electrode (~0.31 V vs Li+/Li0) eliminates anode impedance
Ultra-low mass loading removes electrolyte @ cathode impedance and amplifies diffusion and interface
Li+ electrolyte @ separator
Cathode
Li+ electrolyte @ cathode
Li+ anode interface
Li+ anode diffusion
Anode
Li+ electrolyte @ anode
e- wire
e- anode
e- cathode
Li+ cathode interface
Li+ cathode diffusion

## Slide 9: Cell Tester
Most cell tester requirements are easily achievable
Coin cell reference electrodes require complete shielding
Many cell testers qualify for everything except for rapid low current pulse initiation
Chart: Time (s)
| 0 | 1.7999999544908718E-3 | 1.9999999493904852E-3 | 5.1999998686289572E-2 | 0.10199999742319044 | 0.15199999616008952 | 0.20199999489699039 | 0.25199999363388947 | 0.30199999237079034 | 0.35199999110768943 | 0.40199998984459029 | 0.45199998858149115 | 0.50199998731839024 | 0.5519999860552911 | 0.60199998479219019 | 0.65199998352909105 | 0.70199998226599014 | 0.751999981002891 | 0.80199997973969062 | 0.8519999784765897 | 0.90199997721349057 | 0.95199997595038965 | 1.0019999746872905 | 1.0519999734241896 | 1.1019999721610905 | 1.1519999708979896 | 1.2019999696348904 | 1.2519999683717895 | 1.3019999671086904 | 1.3519999658455895 | 1.4019999645824903 | 1.4519999633193894 | 1.5019999620562903 | 1.5519999607931911 | 1.6019999595299907 | 1.6519999582668898 | 1.7019999570037907 | 1.7519999557406898 | 1.8019999544775906 | 1.8519999532144897
 | 0 | 0 | 3.6638 | 3.6657 | 3.6638 | 3.6632 | 3.6638 | 3.6689 | 3.667 | 3.6606 | 3.66 | 3.6695 | 3.6664 | 3.6645 | 3.6632 | 3.6683 | 3.6587 | 3.667 | 3.667 | 3.6683 | 3.6664 | 3.6625 | 3.6632 | 3.6657 | 3.6702 | 3.6638 | 3.66 | 3.6683 | 3.6638 | 3.6632 | 3.6606 | 3.6613 | 3.6581 | 3.6645 | 3.6657 | 3.6676 | 3.6632 | 3.6657 | 3.6625 | 3.6676
BioLogic VMP-3e

## Slide 10: Model
A “complete” pulse is one that reaches a steady state
Model expressed in relative, dimensionless units
Many methods only use infinite-volume models approximating the pulse start ()
Relative Change in Capacity:
Relative Change in Potential:
Relative Diffusivity:
Relative Resistance:
Geometric Constants (sphere):
Traditional GITT
AMIDR

## Slide 11: Model
A pulse can be expressed in terms of and which is far better suited for data fitting
Now and are normalized by , the ideal change in capacity suggested by the measured voltage
Adjusting and minimizes error in and equal weight will be given to the start and end of the pulse
Relative Change in Capacity:
Relative Change in Potential:
Relative Diffusivity:
Relative Resistance:
Geometric Constants (sphere):

## Slide 12: Protocol
Complete pulse time = complete relaxation time
Small V limit spacing ensures consistent , low current ensures complete pulses
Within pulses, data should be collected logarithmically to get even distribution over
Parameters | V Limit Spacing | Rate | Rest Time
4.2 – 3.7 V | 25 mV | C/40 | 1 hour
3.7 – 3.5 V | 25 mV | C/120 | 4 hour
3.5 – 3.7 V | 10 mV | C/300 | 4 hour
3.7 – 4.2 V | 25 mV | C/40 | 1 hour
NM9505

## Slide 13: Error Management
Generally, if diffusivity between charge and discharge do not agree, something went wrong
Misalignment of after relaxation potentials detects undesired side reactions
Rapid changes occur at H2-H3 phase transitions and incomplete pulses/rests occur at low SOC
Dch
Ch
NMC811
NM9505
NM9505

## Slide 14: Error Management
Generally, if diffusivity between charge and discharge do not agree, something went wrong
Misalignment of after relaxation potentials detects undesired side reactions
Rapid changes occur at H2-H3 phase transitions and incomplete pulses/rests occur at low SOC
Dch
Ch
Figure adapted from [1] S. Kang and W. Chueh, “GITT Reinvented” J. Electrohem. Soc., 168, 120504 (2021)
NM9505

## Slide 15: Error Management
Generally, if diffusivity between charge and discharge do not agree, something went wrong
Misalignment of after relaxation potentials detects undesired side reactions
Rapid changes occur at H2-H3 phase transitions and incomplete pulses/rests occur at low SOC
Dch
Ch
Figures adapted from [1] S. Kang and W. Chueh, “GITT Reinvented” J. Electrohem. Soc., 168, 120504 (2021)
NM9505
!

## Slide 16: Results
Kinetics are good at all SOC except low SOC
decreases and increases rapidly at low SOC
measured by fitting with AMIDR is more accurate than a more traditional method, measuring the initial voltage drop which may be underestimated due to capacitance
Dch
Ch
NM9505

## Slide 17: Results
NM9505
, chemical diffusivity, the measurement that physically describes Li transport, is inversely related to
When is low, there is a large difference in enthalpy of occupation sites between high and low concentration, further driving diffusion and shrinking concentration change
When is low, small concentration changes incur large overpotentials, so total overpotential is similar
Dch
Ch
, free-path tracer diffusivity, an abstract proxy for site hopping activation energy, is constant except for low SOC
Site hopping typically occurs via divacancy hopping, which has a low activation energy
When divacancy hopping is unavailable, high activation energy single vacancy hopping occurs

## Slide 18: Results
Commercial high-Ni active materials have similar profiles where the high-Mn active material differs
At most SOC, High-Mn materials have poor diffusion kinetics due to their high Ni in the Li layer () reducing available divacancies
At low SOC, all layered oxides have similar poor diffusion kinetics because divacancies are uncommon regardless of
All commercial active materials share similar interface contact resistivity () profiles
is normalized by active material surface area
AMIDR cannot determine whether is due to a single charge transfer reaction or a thin, low surface layer

## Slide 19: Conclusions
AMIDR is a powerful method and program available at github.com/MitchBall/AMIDR for reliably measuring active material diffusivity and interface resistance. Even if you don’t use AMIDR, helpful tips to improve your diffusivity measurements include:
Make cells with low mass loading to amplify diffusion impedance
Measure complete pulses to ensure relaxations are also complete
Measure both charge and discharge
Be rigorous!
  Your measurement is only as good as your worst source of error
Cell Tester
Protocol
Model
Cell Design
Error Management

## Slide 20: Future Work
Measure Na/K-ion active materials
Requires a Na/K-ion reference electrode
Calculate average site hopping activation energy
More tests must be performed at different temperatures
Better measure high regions (plateaus)
Will require more V accuracy, less sampling frequency, perhaps a different cell tester

## Slide 21: Thanks!
Dahn-Yang-Metzger Lab Members
The authors acknowledge Tesla Canada and NSERC for funding this work
Questions?

## Slide 22: References
[1] S. Kang and W. Chueh, “GITT Reinvented” J. Electrohem. Soc., 168, 120504 (2021)

## Slide 23: Particle Size Variation (Bonus)
AMIDR is robust against particle size variation
Exact model for bimodal material cannot be developed, but start and end approximations can
Particles of 1 and 3 arb. units in a 1:1 capacity ratio share a similar profile to a uniform model

## Slide 24: Charge/Discharge Disagreement (Bonus)
Limited charge/discharge disagreement is due to change
Reducing the V limit spacing reduces this error
Parameters | V Limit Spacing | Rate | Rest Time
4.2 – 3.7 V | 25 mV | C/40 | 1 hour
3.7 – 3.5 V | 25 mV | C/120 | 4 hour
3.5 – 3.7 V | 25 mV | C/120 | 4 hour
3.7 – 4.2 V | 25 mV | C/40 | 1 hour
Parameters | V Limit Spacing | Rate | Rest Time
4.2 – 3.95 V | 12-13 mV | C/80 | 1 hour
3.95 – 3.7 V | 12-13 mV | C/80 | 1 hour
3.7 – 3.5 V | 12-13 mV | C/240 | 4 hour
3.5 – 3.7 V | 10 mV | C/300 | 4 hour
3.7 – 3.95 V | 12-13 mV | C/80 | 1 hour
3.95 – 4.2 V | 12-13 mV | C/80 | 1 hour
(a)
(b)

## Slide 25: Anode Impedance (Bonus)
Some anode impedance may be acceptable, but its error is measurable
When cathode kinetics are poor, anode impedance is negligable